## Slide 1: Simulation and Analysis of Electrochemical Systems
PhD Defense of
Michael S. Emanuel
in Applied Mathematics
Monday April 28, 2025
PhD Committee:
Chris H. Rycroft • Michael J. Aziz • Boris Kozinsky
michael.s.emanuel@gmail.com github.com/memanuel/PhD-Thesis linkedin.com/in/michael-emanuel
Notes: Slide numbers check the font type

## Slide 2: Overview

## Slide 3: Four Scientific Works
1: Redox Flow Battery Twin
3: Acid- Base Generator
4: Quinone CO2 Capture
2: State of Charge Mapping
3
Simulation
Analysis
Flow Batteries
Carbon Capture
1 RFB Twin
2 SOC Map
4 QCC
3 ABG
Key
Notes: RFB - main research focus
CCS – serendipitous collaborations

## Slide 4: What is a Redox Flow Battery (RFB)?
4
pH
[HA] (mM)
Potential (V)
Charge Movement
Charge battery by moving charge “uphill” to higher potential.
Redox Flow Battery being charged.
1 RFB Twin
2 SOC Map
Notes: The posolyte and negolyte redox reactions have a voltage difference, i.e. E○neg < E○pos. These are material properties.
The negolyte (Q) is reduced to H2Q (reduction means gaining electrons). The posolyte (V4+) is oxidized to V5+ (oxidation means losing electrons)
Electrons flow from anode to cathode. Protons flow through the CEM

## Slide 5: Why Redox Flow Batteries?
5
Energy Information Administration.
Solar and wind are the cheapest, cleanest electricity today…
But they are intermittent: we need energy storage
Redox Flow Batteries (RFBs) are a promising energy storage technology
Decouples energy and power capacity; ideal for grid scale, long duration energy storage
Crimson Energy Storage in CA, 1400 MWh; largest BESS project to go live in the US in 2022 (Recurrent Energy)
1 RFB Twin
2 SOC Map

## Slide 6: Why Carbon Capture & Storage (CCS)?
6
The Palisades Fire engulfs homes in the Pacific Palisades neighborhood of Los Angeles. (Ethan Swope/AP)
Petra Nova CCS facility at NRG WA Parish plant in TX. (Recurrent Energy)
Climate change is real
Carbon Capture & Storage (CCS) can be effective today for capturing flue gas...
And might allow future generations to repair Earth’s climate
4 QCC
3 ABG

## Slide 7: Digital Twin for Porous Electrodes in RFBs
7
Direct numerical solution of governing PDEs
Phenomena—fluid flow, mass transport, electrochemical reaction
Unprecedented scale— 800M cells, 1.25 μm
SOC—state of charge (fraction of available energy stored locally)
M. S. Emanuel, C. H. Rycroft, Digital Twin for Porous Electrodes in Redox Flow Batteries. arXiv (planned submission to Physics of Fluids). DOI 10.48550/arXiv.2502.08034.
SOC
1 RFB Twin
Magnum Opus
Notes: Magnum opus – 4 years Direct numerical solutions of the governing equations.
Incompressible flow: Navier-Stokes equation. Mass transport: Nernst-Planck equation. Chemical kinetics: Butler-Volmer equation. Electrostatics: Poisson equation

## Slide 8: Calculating State of Charge from Image Data
8
Commercial porous electrode was imaged
Reduced species is brighter than oxidized species
But SOC calculations failed: shadows, nonlinear response, misalignment
Model of light production and optical transfer
pH
[HA] (mM)
D. Xi, Y. Zheng, M. S. Emanuel, P. Zhao, M. J. Aziz, Electrochemical Acid-Base Generators for Decoupled Carbon Management. Energy & Environmental Science.
SOC (% max)
0
100
50
200 μm
2 SOC Map
Salvaging a manuscript.
Notes: Our manuscript was languishing unpublished and performed an iterative calibration
The results were good!

## Slide 9: Simulating an Acid-Base Generator
9
Simulation of Acid-Base Generator (Dawei Xi)
Mass transport in 2D
Crossover—problem where species crosses into the “wrong” chamber
Computational answer to an engineering question about crossover
pH
[Na+] (mM)
D. Xi, Y. Zheng, M. S. Emanuel, P. Zhao, M. J. Aziz, Electrochemical Acid-Base Generators for Decoupled Carbon Management. Energy & Environmental Science. DOI 10.1039/D4EE05109B.
NaA flows to right
Electric Field
Lx = 11.18 cm
Ly = 0.10 cm
Na+
H+
H+
3 ABG
“COMSOL doesn’t work!”
Notes: Sodium acetate flows left to right. Electric field points up; this pushes sodium ions up to generate strong base.
Simulating mass transport with Nernst-Planck Eq. Called in after “COMSOL doesn’t work”
A = acetate (CH3COO-).

## Slide 10: Thermodynamic Analysis of a Quinone CCS
10
pH
[HA] (mM)
Quinone based CCS system (Kiana Amini)
Two capture mechanisms, pH swing and nucleophilic swing
“Simple” thermodynamic calculation can explain their relative importance
Solved equilibrium simple numerical techniques
Conclusion: three regimes varying by dominant capture mechanisms
K. Amini, T. Cochard, Y. Jing, J. D. Sosa, D. Xi, M. Alberts, M. S. Emanuel, E. F. Kerr, R. G. Gordon, M. J. Aziz, In Situ Techniques for Aqueous
Quinone-Mediated Electrochemical Carbon Capture and Release. Nature Chemical Engineering. DOI 10.1038/s44286-024-00153-y
4 QCC
“I have a problem…”
Notes: Kiana: “I need help” with a system of equations—scipy optimizer isn’t working.
Solved in two days using a few simple tricks.
Resulting analysis was Figure 1 of published work

## Slide 11: 1. Digital Twin for Porous Electrodes in Redox Flow Batteries
1 RFB Twin

## Slide 12: Simulation Overview of Redox Flow Battery
12
Simulated the porous electrode at the cathode (dashed red rectangle) while the battery is charged.
Membrane is at a constant voltage
Current collector held at a lower, applied reducing voltage, Var
Porous electrode also at Var
This drives reduction of Q to H2Q
H+ crosses CEM, balancing charge
pH
[HA] (mM)
Digital Twin for Porous Electrodes in Redox Flow Batteries.
Notes: The posolyte and negolyte redox reactions have a voltage difference, i.e. E○neg < E○pos
The negolyte (Q) is reduced to H2Q (reduction means gaining electrons)
The posolyte (V4+) is oxidized to V5+ (oxidation means losing electrons)
Electrons flow from anode to cathode
Protons flow through the CEM

## Slide 13: What is AQDS (Anthraquinone Disulfonate)?
13
pH
[HA] (mM)
Digital Twin for Porous Electrodes in Redox Flow Batteries
Aqueous organic: dissolves in water, carbon based
Redox active: undergoes a reversible electrochemical reaction…
Desirable properties:
  Fast kinetics
  High solubility in water
  Long lifetime
  Earth abundant elements
Discovered by Aziz-Gordon collaboration [2014]
Notes: Coupled two electron, two proton transfer (PCET)

## Slide 14: Experiment with a 3D Printed Electrode
14
Architected electrodes were 3D printed and electroplated (Ni, Au)
Known, regular “logpile” geometry
Commercial electrodes—tangle of fibers
Imaged in 3D using confocal microscopy
Gold wires at a reducing voltage Var < 0
Task: simulate in 3D at a sub-fiber scale
D. M. Barber, S. Edgar, M. S. Emanuel, M. D. Nelwood, B. Y. Ahn, B. Román-Manso, T. Cochard, J. Platero, K. Amini, C. H. Rycroft, S. Rubinstein, M. J. Aziz, J. Lewis, Print-and-Plate Architected Electrodes for Electrochemical Transformations Under Flow. Advanced Functional Materials. DOI 10.1002/adfm.202419748.
Notes: Schematic of experiment. Fluid flows left to right (x-axis). Fiber diameter ≈ 35 μm Membrane at z=0 and has voltage φ = 0.
Comment on interplay between experiment and simulation – complement each other.

## Slide 15: Loosely Coupled Problems & Discretization
15
Fluid Flow
Navier-Stokes equation
Incompressibility condition
Chorin Projection Method
Electrochemistry
Nernst-Planck equation (transport)
Butler-Volmer equation (kinetics)
Fixed-Point Iteration
Coupled
Decoupled
Numerical Methods
AMReX Library
Cut cells with implicit boundary
Algebraic Multigrid solvers (HYPRE)
Highly scalable MPI program
Example of cut cells and mesh refinement in 2D
Steady State
Main concern for RFBs
Faster to simulate than full dynamics

## Slide 16: Fluid Flow: Navier-Stokes Equation
16
Navier Stokes equation
Incompressibility condition
2D cross section of fluid speed
2D cross section of fluid pressure
Term | Concept | Units
ρ | Fluid density (constant scalar) | kg·m-3
μ | Dynamic viscosity (constant scalar) | Pa·s
u | Fluid velocity (vector field) | m·s-1
p | Fluid pressure (scalar field) | Pa
Speed (cm/s)
SOC

## Slide 17: Mass Transport: Nernst-Planck Equation
17
Term | Concept | Units
u | Steady state fluid velocity | m·s−1
Dj | Diffusivity of species j | m2·s−1
zj | Charge number of species j | 1
Cj | Concentration of species j | mol·m-3 = mM
Sj | Chemical source term of species j | mol·m-3·s−1
φL | Electrical potential in liquid electrolyte | V = Joule·Coul−1
F | Faraday’s constant | Coul·mol−1
R | Ideal gas constant | Joule·mol−1·K−1
T | Absolute temperature (Kelvin) | K
Regular cells (all fluid)
Covered Cells (all solid)
Cut Cell

## Slide 18: Boundary Conditions & Simulation Overview
18
Applied pressure and fixed concentrations at inlet
Pressure drop drives the flow left to right
No-Slip condition at bottom, top, left, right walls
Membrane at bottom: no slip and zero potential, φL = 0
Wires: no slip, applied reducing potential φS < 0
Digital Twin for Porous Electrodes in Redox Flow Batteries.
Notes: Lower pressure at outlet
Wire Surface: Electrochemical reaction, conversion from oxidized to reduced creates a flux

## Slide 19: Nernst Equation and Overpotential
19
The Nernst equation gives equilibrium potential Eeq vs. reference potential E0 as concentration varies
η is called the overpotential
O: oxidized species R: educed species
Sign convention: Var is “reducing voltage.”
A larger reducing voltage drives reduction (charging)
Reducing Voltage vs. State of Charge
Notes: As SOC increases, it’s harder to add charge.
The vertical gap is the overpotential η.

## Slide 20: Reaction Kinetics: Butler-Volmer Equation
20
Typically, we assume a perfectly reversible reaction, i.e. αO = αR = 0.5, so
Term | Concept | Units
O | Generic oxidized species, e.g. quinone Q | —
R | Generic reduced species, e.g hydroquinone H2Q | —
S | Chemical source term; concentration change rate | mol·m−3·s−1
a | Specific area of solid-liquid interface | m−1 = m2/m3
k0 | Reaction rate constant | m·s−1
αj | Charge transfer coefficient of species j | 1
η | Activation overpotential | V
Stylized Source vs. Overpotential
Notes: Exchange current – how fast does reaction happen forward and backward at the same speed. Analogy: restaurant with people entering and exiting.

## Slide 21: Model Overview: Three Levels of Fidelity
21

## Slide 22: Good Agreement with Experiments
22
Print-and-Plate Architected Electrodes for Electrochemical Transformations Under Flow.
a) Fluorescence data of logpile electrode at three slices; background is subtracted
b) Calibrated experimental SOC
c) Corresponding simulated SOC
Note good qualitative agreement with build-up of high SOC above vertical and horizontal wires, and in convective tails coming off them

## Slide 23: Electromigration is Negligible – Model Refinement
23
Simulation of a logpile geometry; cross section at mid-plane
(a) state of charge; reduced species builds up and spreads out due to diffusion as flow moves through electrode
(b-c) potential in electrolyte is negligible, max of 0.47 mV
(d) special model is very close to full BV, RMSE just 8.6E-4
a
c
d
State of Charge
SOC Difference: Special vs. BV
Electrolyte Potential ϕL
b
c

## Slide 24: Iterative Upsampling: “Multigrid on Steroids”
24
2.5 mm/s
0.0 mm/s
Box = 4.0 μm
Box = 2.0 μm
Box = 1.0 μm
Box = 0.5 μm
Fluid simulation of a 100 μm diameter single wire in an open channel of 1.0 x 1.0 mm
Resolution doubles at each step
Each simulation is initialized with results of the coarser resolution
Convergence time improved from 41 hours to under one hour
M. S. Emanuel, Simulating Porous Electrodes in Redox Flow Batteries. APS DFD talk, 21Nov2023.
Notes: Fluid enters the inlet at 2.8 mm/sec
Simulation has fully converged at the finest resolution

## Slide 25: Steady State PDE in Terms of State of Charge s
25
Simplified Nernst-Planck at steady state in terms of s
In electrolyte interior, advection balances diffusion
On electrode surface, the reaction balances diffusion
σ is the sigmoid function
and are nondimensionalized voltage & overpotential
Notes: Total electroactive concentration is a constant under modest assumptions; all concentrations known from the state of charge s
Analogy – merging onto a highway. How fast traffic moving on the pike = advection. Merging in = diffusion.
Total electroactive concentration 𝑐0 is a constant under modest assumptions; all concentrations known from the state of charge s
Analogy – merging onto a highway. How fast traffic moving on the pike = advection. Merging in = diffusion.

## Slide 26: Nernst Model
26
Given the SOC field, obtain new estimate of overpotential to balance reaction vs. diffusion
Iteratively refine overpotential η and SOC s on electrode surface; ω small relaxation parameter
Then update s on interior with advection and diffusion terms
Continue until convergence criteria met

## Slide 27: Results: Fluid Flow Streamlines
27
Flow Speed (cm/s)

## Slide 28: Results: Overpotential on Electrode
28
Overpotential (mV)

## Slide 29: 2. Calculating SOC from Images of a Commercial Porous Electrode
2 SOC Map

## Slide 30: QEFSM Experimental Setup
30
Microfluidic flow cell compatible with electrochemistry and confocal microscopy. A) Exploded view of the individual components with labeled coordinates. B) Images of assembled cell from above (top) and below (bottom). Working electrode visible in bottom image. C) Widefield optical microscopy image of commercial AvCarb MGL 190 electrode.
A. M. Graf, T. Cochard, K. Amini, M.S. Emanuel, S. M. Rubenstein, M. J. Aziz, Quantitative Local State of Charge Mapping by Operando Electrochemical Fluorescence Microscopy in Porous Electrodes. Energy Advances.

## Slide 31: Fluorescence Difference of AQDS Redox Pair
31
Quantitative Local State of Charge Mapping by Operando Electrochemical Fluorescence Microscopy in Porous Electrodes.
Emission spectra of 40 mM AQDS solutions vs. wavelength λ at different SOCs obtained from excitation wavelength λex = 405 nm. Shaded rectangle—accepted range of green band-pass filter.
Raw intensities integrated over shaded region of (B) vs. SOC. Solid lines: theoretical concentration fraction of each species from dimer model.
Notes: Reduction scheme of AQDS to H2AQDS via PCET (top). Dimer formation (bottom).
Note significant amount of dimer at 50% SOC leading to a decidedly nonlinear response of brightness vs. SOC.

## Slide 32: Modeling Brightness vs. Concentrations
32
28 operating images (4 concentrations x 7 voltages)
One bright calibration image at high, uniform SOC
Challenges: shadows, misalignment, nonlinear response
Light production model
Optical model
AQ, H2AQ and QH are oxidized, reduced and dimer
Indices r for reaction condition, i for pixel

## Slide 33: Calculating SOC from Brightness
Optical factors: from bright image,
Brightness coefficients: C = [α; β; γ; δ]
Weighted Concentration:
Regress (by mean on 28 runs)
Iterate brightness: regress (by pixel)
Iterate factors: regress (by run)
33
I
X
C
=
N x 1
N x 4
4 x 1
Regression for C
I
P
F
=
28 x 1
28 x 1
1 x 1
Regression for Fi
Notes: Solve all concentrations from y = [H2AQ] / CT
Dimensionless dimer coefficient, R = Kdim CT
Solution: ,
Solve all concentrations from y = [H2AQ] / CT
Dimensionless dimer coefficient, R = Kdim CT
Solution: 𝑥= ((1−𝑦))/((1+2𝑅𝑦)), 𝑧= (𝑅𝑦(1−𝑦))/((1+2𝑅𝑦))

## Slide 34: QEFSM Results—Minimal Visual Artifacts
34
Quantitative Local State of Charge Mapping by Operando Electrochemical Fluorescence Microscopy in Porous Electrodes.
Local SOC from image data
A) Steady state SOC maps under varying conditions. B) Histograms of SOC distribution over valid pixels for each image.
Note significant departures from linear gradient predicted by mean-field theory.
Notes: Applied overpotential increases left to right (50, 100, 175 mV). Total AQ concentration increases top to bottom (10, 20, 30, 40).
White pixels are fibers / impurities.

## Slide 35: 3. Simulating an Acid-Base Generator
3 ABG

## Slide 36: pH Swing Mechanism for Carbon Capture
36
M — generic metal ion with +1 charge, e.g. sodium
A — conjugate base a generic acid with −1 charge, e.g. acetate (CH3COO−)
Basic solution absorbs carbon dioxide to form carbonate and bicarbonate
Carbon dioxide is released when this solution is later acidified
Notes: The ocean is mildly alkaline and is a huge CO2 sink.

## Slide 37: Acid-Base Generator Cell Structure
37
D. Xi, Y. Zheng, M. S. Emanuel, Z. Panlin, M. J. Aziz, Electrochemical Acid-Base Generators for Decoupled Carbon Management. Energy & Environmental Science.

## Slide 38: ABG Schematic & Simulation Approach
38
Flow Field
Unfurling serpentine flow path to x-axis
Schematic; x-axis is flow direction, y-axis small space between anode and cathode

## Slide 39: Explicit Time Steps for ABG Simulation
39
Plane Poiseuille flow (analytical solution)
Nernst-Planck equation for mass transport
Membrane boundary condition: electromigration replaces H+ with Na+
Uniform electric field from anode to cathode, E0 = Vapp / Ly
Explicit step—advection, diffusion, electromigration operators
Electroneutrality imposed; r = ρ+ / ρ−, f = , concentrations adjusted by r
Chemical equilibria solved—water and acetic acid dissociation
Notes: Steady state obtained by iterating until convergence

## Slide 40: Acid-Base Generator Simulation Results
40
Simulation validates Dawei’s engineering design
High H+ concentration at top would indicate crossover…
There is negligible crossover attributable to mass transport as described by Nernst-Planck
Experimental findings of low crossover; hypothesis – due to membrane effects
Tractable with appropriate modeling assumptions
Difficult to get this level of intuition from experiments
pH
[H+] (mM)
Electrochemical Acid-Base Generators for Decoupled Carbon Management
[Na+] (mM)
NaA flows to right
Electric Field
Na+
Electric Field
Negligible H+
H+
H+
Notes: When H+ crosses over, H+ mixes with OH- to make water and heat. Bad!
Could not be readily simulated in COMSOL. Comparable works in literature lack simulations of this kind
.

## Slide 41: 4. Thermodynamic Analysis of a Quinone Carbon Capture System
4 QCC

## Slide 42: Thermodynamic System of Equations (9)
42
Kiana’s Problem:
Chemical equilibria (7)
Electroneutrality
Quinone conservation
Problem: optimization in scipy doesn’t work!

## Slide 43: Strategy for Optimization Problems
43
Eliminate variables
Nondimensionalize physical quantities
Rescale variables to mean near zero, variance near one
Map constrained variables to the real line:
  E.g. if x > 0, use ln(x)
  E.g. if x in (0, 1), use
Use 2-norm composite error function, e.g.
Use a neutral initial guess

## Slide 44: Eliminating Variables
44
Operating conditions:
Inorganic concentrations: M+, H+, OH-, CO2 (aq), HCO3-, CO32-
Organic concentrations: AQH2, AQH-, AQH2-, AQH(CO2)2
Solve inorganic concentrations in terms of [H+]:
Solve organic concentrations in terms of [AQH2]:
Left with two variables, [H+] and [AQH2]
Manipulate state variables to minimize composite error

## Slide 45: Transforming Variables & Calling Optimizer
45
Two state variables, [H+] and [AQH2]
Apply transformations to state variables
Define errors—electroneutrality, quinone conservation, and composite
Optimizer: minimize composite error by adjusting x and y

## Slide 46: Results: Three Behavioral Regimes
46
In Situ Techniques for Aqueous Quinone-Mediated Electrochemical Carbon Capture and Release.
Concentrations of HCO3−, CO32−, CO2 (aq) and AQ(CO2)22− at different KAQ-adduct values. Gray region: pH swing dominates. Blue region: nucleophilicity swing dominates. Red region: both mechanisms in play.
Understanding dominant behavior leads to better molecular engineering strategies.
Notes: (a-c): Equilibrium concentrations by solving equations.
Total concentration of 0.2M AQ with K4 = 1.1E−6, K5 = 4.1E−10, Kw = 1.0E−14.

## Slide 47: Conclusions & Future Research Directions

## Slide 48: Scientific Conclusions
48
Modeling steady state easier than integrating dynamics
Any mass transport system can be modeled at steady state by switching from flux to boundary value condition
Useful to have a series of related models on same back-end with increasing levels of fidelity
Porous electrodes in flow batteries are typically run in the Stokes flow regime with negligible electromigration
A porous electrode geometry can be evaluated with a single flow simulation plus a handful of reaction simulations
We can do computational design of electrodes!

## Slide 49: Comments on Scientific Computing
49
We should broaden our ambitions in the exascale age of massive scientific supercomputers
Direct numerical simulations of PDEs are now within reach
Explicit methods are often underappreciated
Applied mathematicians should collaborate across disciplines more…
But institutional support and incentives are lacking
Data analysis is now a specialty and should be treated as such
Notes: Yoda: “You must unlearn what you have learned.”

## Slide 50: Future Research Directions
Digital twin for active learning and surrogate ML models
Darcy mosaic model: 3D grid of box-shaped tiles
  Coupled hydraulically by Darcy flow
  Coupled electrochemically by SOC values on shared faces
Mass transfer coefficient km as emergent vs. phenomenological
50

## Slide 51: Acknowledgments

## Slide 52: Advisors: Chris Rycroft & Mike Aziz
52
Advisor:
Chris H. Rycroft
Co-Advisor:
Michael J. Aziz
U.S. Department of Energy Office of Basic Energy Sciences Grant DE-SC0020170

## Slide 53: Rycroft Group
53

## Slide 54: Aziz Group
54

## Slide 55: Convexity Colleagues
55

## Slide 56: Old Friends
56

## Slide 57: Gibson Family
57

## Slide 58: Emanuel Family (OG)
58

## Slide 59: My Family
59

## Slide 60: Afterword: Responding to a Time of Crisis in America

## Slide 61: Defending Harvard Against Tyranny
61
Harvard is under attack by our own government
Trump wants to control who we hire, what we teach, and even what we think
As a Jewish American student, I know antisemitism is a real problem, but I say to Trump and his thought police: You do not speak for me when you attack Harvard. We are confronting our problems together, as a community of scholars, students and researchers. Stay out of it.
To the rest of you I say: Please stand with me to defend Harvard against this unjustified and un-American attack!

## Slide 62: Sustaining Science at Harvard and Beyond
62
Harvard may ultimately prevail in litigation, but not for years
Even the Harvard endowment cannot fund our research
We won’t be able to flip a switch and “turn science back on”
A handful of influential philanthropists could sustain science at Harvard until we emerge from this crisis
I have one foot in each of the worlds of finance and science
Even a modest gift could have a transformational impact
If you or someone you know can help, please contact me! (michael.s.emanuel@gmail.com)

## Slide 63: Appendix

## Slide 64: Teasers to Read Dissertation
64
Dedication and acknowledgments
Epigraphs—textual, musical (!) and youthful
Details—conceptual, numerical and experimental
Foreword—personalized overview of my research
Introduction—larger scientific context of my work
Afterword—addressing the crisis in American science

## Slide 65: Image URLs
65
https://www.eia.gov/todayinenergy/detail.php?id=56880
https://www.energy-storage.news/us-installed-grid-scale-battery-storage-capacity-reached-9gw-25gwh-in-record-breaking-2022/
https://www.npr.org/sections/the-picture-show/2025/01/13/g-s1-42407/see-california-wildfire-devastation-pictures-altadena-eaton-palisades
https://www.catf.us/resource/carbon-capture-storage-what-can-learn-from-project-track-record/
https://en.wikipedia.org/wiki/Quinone